VIRIDIAN VFLOAT SUPERCLEAR™ TC

Glass shall be Viridian VFloat SuperClear™ TC		 * thick,			  (Annealed, Heat Strengthened, Toughened and/or Laminated. Please nominate in this section your requirements.)

* Glass Thicknesses available:

- Annealed Glass: 4mm, 6mm, 8mm, 10mm, 12mm, or 15mm 	- Toughened: 4mm, 6mm, 8mm, 10mm 12mm, or 15mm

- Heat Strengthened: 4mm, 6mm, 8mm, 10mm or 12mm

- Laminated Glass: 8.38mm to 31.52mm

The glass shall comply with the following performance criteria:

| Visible Light Transmission % | U Value | Shading Co-efficient (SC) | Solar Heat Gain Coefficient (SHGC) |
| --- | --- | --- | --- |

Solar control glass may be subject to thermal stress and should therefore be thermally assessed prior to installation.

Heat Soaking - All toughened glass products must be heat soak tested.

Heat soak testing is a destructive test, which reduces the likelihood of spontaneous breakage by converting impurities such as nickel sulphide inclusions.

Heat Strengthening -All glass which requires extra strength and thermal resistance will be heat strengthened. Heat strengthening increases the strength of annealed glass; however it is not a substitute for toughened glass.

In the event of fracturing heat strengthened glass will crack and tends to remain in glazed position.

All glass is to be selected and installed in accordance but not exclusively with the following Australian and/or New Zealand Standards

- AS 1288 Glass in Buildings Selection and Installation

- AS 1170 Minimum Wind Loads on Structures

- AS/NZ 2208 Safety Glazing Materials in Buildings

- AS/NZ 4666 Insulating Glass Units

- AS/NZ 4667 Quality Requirements for cut-to-size and Processed Glass